| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: Margot Phelps | 01/13/11 | V2 | E1100040-x0 |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

A gold coating is to be deposited onto the barrel of the Compensation Plate, with some areas masked off to create the pattern specified below. The Compensation Plate (CP) is a cylindrical fused silica substrate, 340 mm diameter x 100 mm thick; see LIGO-D1000979-v2 for the detailed drawing of the CP.

Applicable Documents

LIGO-D1000979-v2 Advanced LIGO COC TCP Substrate Drawing

LIGO-D0900981-v2 Thin Compensation Plate Barrel Coating Pattern

LIGO-D080177-v4 Compensation Plate Face Coating Pattern

Coating Specifications:

Side S3 (refer to D1000979-v2) is to be coated. Coating is to cover the full barrel (S3) of the optic (except on masked areas), extending up to the chamfer (no coating on the chamfer).

Underlayer: 500 Angstroms (nominal) of inconel or other suitable material to provide adhesion.

Gold coating: 1000 Angstroms (nominal) gold.

Uniformity: Coating thickness should be uniform to approximately 25%.

Masking: Two rectangular areas are to be masked off (not coated). The size and location of these areas are defined in LIGO-D1000981.

Durability: The coating must be able to withstand soldering, using an Indium-Silver solder, at a temperature of 220-240 deg C.