| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | D. Coyne | 11-30-06 | E060269 | A | 11-30-06 |

Applicable Documents

LIGO-D060513-A  	Fused Silica Substrate, Advanced LIGO Pathfinder 
LIGO-D050337-A  	Fused Silica Blank, Input Test Mass 
LIGO-E050071-C  	Fused Silica Blank, Input Test Mass

Requirements

Polished surfaces shall appear transparent with no grey, scuffs or scratches visible to the naked eye when viewed in normal room light against a black background.

Physical Configuration

According to LIGO-D060513-A   Fused Silica Substrate, Advanced LIGO Pathfinder

Fabricate from

LIGO-D050337-A  	Fused Silica Blank, Input Test Mass 
LIGO-E050071-C	Fused Silica Blank, Input Test Mass

Bevel

Bevel for safety per D060513

Serial Number

Serial Number “PF X” shall be written in indelible ink on the barrel of the optic, where X is specified by Caltech when the material is delivered from LIGO to vendor.

Registration Marks

A registration arrow shall be drawn in indelible ink on the barrel of the optic, pointing toward Surface 1.  This mark is used to reference the top orientation of the delivered data, and for measurement comparison.

Scratches, Sleeks and Point defects

Point defects of radius greater than 25 micrometers are treated like scratches for the purpose of this specification.

Scratches and Sleeks, Surface 1

The total area of scratches and sleeks within the central 120 mm diameter shall not exceed 20 X 103 square micrometers (width times length.)

The total area of scratches and sleeks outside the central 120 mm diameter shall not exceed 500 X 103 square micrometers (width times length.)

Scratches and Sleeks, Surface 2

The total area of scratches and sleeks within the central 120 mm diameter shall not exceed 240 X 103 square micrometers (width times length.)

Point Defects, Surface 1

There shall be no more than 10 point defects of radius greater than 2 m within the central 120 mm diameter.    There shall be no more than 100 point defects of radius greater than 2 m on the entire surface.  Average density of defects less than 2m radius must be less than or equal to 1 per 4mm2

Point Defects, Surface 2

There shall be no more than 100 point defects of radius > 2 m within the central 120 mm diameter

Scratch and Point Defect Inspection Method

1. The surface is examined visually by two observers independently. The examination is done against a dark background using a fiberoptic illumination system of at least 200 W total power. A 100% inspection of the surface is carried out. Pits and scratches down to 2 micrometers in width can be detected using this method of inspection.  Any scratches or sleeks that are detected will be measured using a calibrated eyepiece.

2. Further inspection will be done with a minimum 6X eyeglass using the same illumination conditions, again with two observers. Sleeks down to 0.5 micrometers wide can be detected using this method. The surface will be scanned along one or two chords from centre to edge, then at ten positions around the edge, and ten to fifteen positions near the centre.

3. An inspection is then carried out with a dark field microscope with a similar sampling frequency as described in section 2.

Optical Surface Figure, measured over the central 150 mm diameter

Surface 1:  Spherical, concave. Radius of curvature:  2098 m +36 m, -22 m absolute.   
Reproducibility Goal: 2098 m ± 3 m Requirement: 2098 m ± 9 m
Astigmatism:  < 3 nm Amplitude of the Zernike coefficient Z2,2 as defined in Born and Wolf pp. 523-525.

Surface 2:  Nominally flat. Curvature of the transmitted reflected wavefront off of Surface 1 as measured through Surface 2 must be within ± 15m of the calculated curvature accounting for the bulk of the material.  The calculated curvature is based on the Surface 1 measurement and ideal homogeneous index of refraction.

Surface Error, Low Spatial Frequency: measurement aperture to 1 mm-1

The following root mean square standard deviation (σrms) values are calculated from the phase maps which are to be provided with each optic.  For this calculation the amplitudes for the best fit Zernike terms Z0,0, Z1,1, Z2,0 and Z2,2 or corresponding Seidel aberrations are subtracted from the phase map.  Known bad pixels may be excluded from this calculation.

Surface 1, Frequency Band:  < 1 mm -1 
Measured over the central 300  mm diameter aperture:  σrms < 2.1 nanometers 
Measured over the central 150 mm diameter aperture:  σrms < 0.7 nanometers

Surface 2 - Frequency Band:  < 1 mm -1 
Measured over the central 300 mm diameter aperture:  σrms < 4 nanometers
Measured over the central 150 mm diameter aperture:  σrms < 2 nanometers

Error, High Spatial Frequency:  1– 750 mm -1

Surface 1 HSF error σrms < 0.16 nanometers measured at the following locations: 
1.  Within 2mm of the center of the surface.
2.  Four positions equally spaced along the circumference of a centered, 60 mm diameter circle. 
3.  Three positions equally spaced along the circumference of a centered, 120 mm diameter circle.

Surface 2 HSF error σrms < 0.4 nanometer measured at the following location: 
1.  Within 2mm of the center of the surface.

Inspection

- Table 1: Inspections

| Specification | Test Method | Data Delivered |
| --- | --- | --- |
| Scratches and Point defects | Visual Inspection | Hand sketch including scratch/pit dimensions |
| Figure | Interferometry | Surface phase maps |
| Errors - Low Spatial Frequency | Interferometry | Surface phase maps |
| Errors - High Spatial Frequency | Interferometry | Surface maps for 3 central locations. Numerical values included with certification |

Orientation:  For the purpose of full surface phase maps the substrate shall be oriented such that the registration mark shall be at the top center of the data.

Format:  All Data shall be delivered according to Table 1.  In addition to the hard copy an electronic data set of the phase maps shall be delivered in either ASCII or Vision.OPD format.

# Comments

Loss Budget: 75ppm/FP arm from meeting 10-06-06,

Diffraction 2 * 0.4ppm

Defect Scatter 2 * 3.7ppm (currently 60)

Absorption 2 * 0.5ppm

Surface roughness scatter 2*5ppm

Surface figure 2 * 20ppm

ETM transmission 7ppm

Totals at 66.2

All based on geometric loss from central 120mm diameter

20,000um square = 2 ppm of the total area of the central 120 mm diameter.

LIGO1 AVERAGE total scratch area was 17,000 over 235mm diameter.  There were NO point defects reported in initial LIGO.

Max 1.7ppm of the beam area.  The density requirement limit to max loss of ~2.5ppm

ROCs must be absolute to ±36m, -22 (pf private communication, beam spot not to change by more than 5mm radius) match to …?±?

Hiro suggests 160 aperture from modeling with Yi Pan,

Hiro/YiPan also suggest -3, +1m tolerance to maintain 1% limit on SNR degradation.

NOTE: TCS can only make ROC smaller
up to 2207Km could be corrected

expect to have to change ROC by up to 10K from low to high power.

Chose 2076+22 as the nominal ROC since TCS can only make ROC smaller

ROCs must be absolute to ±36m, -22 (pf private communication, beam spot not to change by more than 5mm radius) match to …?±?

Hiro suggests 160 aperture from modeling with Yi Pan, I have chosen 180 to be consistent with the rest of the document.

Hiro/YiPan also suggest -3, +1m tolerance to maintain 1% limit on SNR degradation.

NOTE: TCS can only make ROC smaller.
Up to 2207Km could be corrected.

LIGO1 spec was ambiguous:

Measured at 690 nm with the wavefront transmitted through Surface 2, passing through the material,

reflected from Surface 1 back along the same path.

Radius of curvature of the wavefront: 9,740 meters +500 meters, -100 meters

Astigmatism: < nanometers (surface peak to valley)

Expect to have to change ROC by up to 10K from low to high power. Back side tolerance is based on 1/10 fraction of this change.

Per T060223, sharp errors of order 20 nm at a position of 3 cm in from the edge have an effect on cavity loss of order ~1ppm

Set at 150 for pathfinder because of the standard instrument size.

160mm diameter comes from HIRO modeling of fabray perot cavity: when outside zone multiplied by three in noise, the cavity loss only changed ~15% or 3ppm

Based on Statistical phase maps Hiro recommends ~.5 nm rms if we want to be sure to be below 30ppm loss due to this type of error.  .5nm rms typically gives rise to ~18ppm loss.

Roughly 2x the central requirement

0.16nm rms ~ 3.6ppm

Compare to budget of 8ppm/mirror and this must include scatter sites…