| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | D. Coyne, Willems | 12-12-06 | E060275-00 | A | 12-12-06 |

Scope

The glass blanks defined by this specification are to be used in research as a LASTI compensation plate.  This is not the final configuration for Advanced LIGO compensation.

Applicable Documents

LIGO - D060527-A Fused Silica Blank, LASTI Compensation Plate

Requirements

Material				Fused silica

Physical Configuration

According to

LIGO - D060527-A Fused Silica Blank, Input Test Mass

Clear Aperture

Central 275 mm

Final Shaping

Shaping shall be performed using a progression of grit size ending with a 320 or smaller grit tool

Defect Depth

Maximum on any surface or corner is less than 0.5 mm

Bubble and Inclusion Cross section

Total ≤ 3 mm2 /100cm3 of Glass within the clear aperture

Inclusions with a diameter of 0.06 mm or less are disregarded

Maximum inclusion diameter

≤ 1.5 mm

Striae

Class 1, Grade A according to MIL-G-174 within the clear aperture

Inspection

Certification of the above requirements must accompany any delivery.