| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | Coyne, Willems | 12-12-06 | E060275-00 | A |  |

Applicable Documents

LIGO-D060534-A	Thermal Compensation Plate
LIGO-D060527-A 	Fused Silica Blank LASTI Compensation Plate
LIGO-E060273-A	Fused Silica Blank, LASTI Compensation Plate

Requirements

Physical Configuration

Shape and Polish according to
LIGO-D060534-A	Thermal Compensation Plate

Fabricate from
LIGO-D060527-A 	Fused Silica Blank LASTI Compensation Plate
LIGO-E060273-A	Fused Silica Blank, LASTI Compensation Plate

Registration Marks

Registration marks shall be etched, ground or sandblasted and located per LIGO- D060534

Serial Number

Serial and Part Numbers shall be etched, ground or sandblasted and located per LIGO- D060534

Side and Bevel Polish

Sides and Bevels shall be polished using a progression of smaller grit sizes.  The last step before final polish shall be equal to or less than a five micrometer grit finish. These surfaces shall appear transparent with no grey, scuffs or scratches visible to the naked eye when viewed in normal room light against a black background.

Surfaces

The optical surfaces, 1 and 2, shall be polished using a progression of smaller grit sizes.  The last step before final polish shall be equal to or less than a five micrometer grit finish.

Surfaces 1 and 2 are to be polished flat to 150 nm peak to valley as measured over the central 120 mm diameter.  Surface finish shall be 40/20 scratch/dig, or better.

Inspections

| Specification | Test Method | Data Delivered |
| --- | --- | --- |
| Outside Diameter | Physical inspection | Measured dimension |
| Wedge | Physical inspection | Measured dimension |
| Thickness | Physical inspection | Measured dimension |
| Flatness, Surfaces 1 and 2 | Interferometry | Interferogram |