| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Name Brian O’Reilly | Ken Mason | 617-324-5250 | ELIGO HAM SEI |  |

| Dwg/Part Number | Rev | Part Description / Material |  | Qty |
| --- | --- | --- | --- | --- |
| D071060 D071061 D071073 D071060 D071140 D071103 D071063 D071067 D071471 D047932 D071105 INA NKX-25 Z | C C C C D C D C C C D | Type 00, AL AL AL Type 01, AL AL AL AL AL Flex Plate, AL AL AL Combination Bearing (no HPD number assigned) SS Nuts with a through hole. Threaded ¾-10 (acme) |  | 2 2 1 1 1 2 1 1 2 2 1 3 3 |

2

| Used In (next higher assembly): |  |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |
| HPD |  |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | clean per E960022: Ultrasonic clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 2/17/08 |
| 2 | Vacuum Bake |  |  | per E960022: 120°C, 48 hrs | T.E. | 2/19/08 |
| 3 | Control Point |  |  | Review/Approve RGA scan | BO’R | 2/19/08 |
| 4 | Wrap & Tag vacuum clean parts |  |  |  | H.O. | 2/20/08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: LLO c/o Ken Mason File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 4/8/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

These are aluminum for the enhanced LIGO HAM SEI . These are spare parts. Hold at LLO, clean as needed, or when ovens have spare capacity

# Footnotes

Standard Liquinox solution is 1 tablespoon in 1 gallon of water.