| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Adam Mullavey |  | 225 686-3139 | OMC, ELIGO |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D070181 D070197 |  | Tip Tilt OSEM Backplate – Left Side Tip Tilt OSEM Backplate – Right Side NB. All parts are aluminium |  | 4 4 |

| Used In (next higher assembly): | OMC |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |
| N |  |  |  |  |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | Per LIGO E960022: -Ultrasonic clean in Liquinox for 10 minutes. -Rinse in distilled water at least 3 times, changing the rinse water every time. | T.E. | 2-17-08 |
| 2 | Vacuum Bake |  |  | Per E960022, Class A, 120ºC for 48 hours | T.E. | 2-25-08 |
| 3 | Control Point |  |  | Review/Approve RGA scan | BO’R | 2-25-08 |
| 4 | Wrap and Tag vacuum clean parts |  |  |  | T.E. | 2-25-08 |
| 5 | Ship and Deliver/File paperwork |  |  | To be used at LLO site. No shipping required. | BO’R | 4-21-08 |