| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: L. BARSOTTI | 01-18-11 |  |  |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: P.FRITSCHEL |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

# Description

2” Ø Flat/Flat high reflector @ 1064nm

# Material

Corning HPFS 7980 1-G

# Dimensions

1"Ø +.000/-.005" X .375" ± .020" tk., Plano / Plano

# Surface Roughness

Side 1

Super polish

Surface Roughness: <1Å RMS in CA

Surface Quality: 10-5

Side 2

Commercial Polish

Surface Roughness: <5Å RMS in CA

Surface Quality: 40-20

# Surface Figure

Side 1

Flat < λ/10 at 632.8 over central 80%

Side 2

Flat < λ/4 at 632.8 over central 80%

# Coating

Wavelength: 1064nm

Angle of incidence: 45°5° (best effort for wider AOI range)

Side 1

R >= 99.995% @ 1064nm (best effort) for s and p-polarization

Side 2

AR coating, R < 1% @ 1064nm (best effort) for s and p-polarization

Serial numbers and registration marks shall be scribed or	etched on the barrel of	the optic for in-vacuum use

# Coating vendor to provide:

  - 1. Three spectrophotometer graphs of the reflectance and transmittance of the HR coatings; one covering the spectrum from 500nm to 1200nm; the others, with increased sensitivity, showing wavelengths from 900nm to 1100nm and from 500nm to 600nm

            - 2. Spectrophotometer graphs of the reflectance of the AR coating taken as cited above.