Title
Adaptive Mode matching for advanced LIGO
Volker Quetschke, Joseph Gleason, Christina Leidel, Michelle Snider, Malik Rakhmanov, Liang Zhang, Guido Mueller, David Reitze, David Tanner
Department of Physics
University of Florida
DCC LIGO-G050422-00-Z
LSC meeting, August 16, 2005
LIGO Hanford Observatory

---
Motivation
Motivation
Interferometric gravitational wave detectors are basically interferometers with suspended components that are operated in vacuum.
Objective:
  - Actuator to change the modal parameters of a Gaussian beam without moving parts.
Requirements:
  - Touch free
  - Vacuum compatible (UHV)
  - Stationary (no movable parts)
Solution:
  - Telescope with lenses with variable focal lengths

---
Principle
Adjustable lenses
Use thermal lensing effect
Use dichroic material
  - high absorption for heating beam
  - low absorption for probe beam
Schott OG515 is highly transmissive for 1064nm and strongly absorbing for 514 nm.
Two laser setup
  - Argon-Ion laser provides heating beam to actuate the lens
  - Nd:YAG laser probes the created effect
Heating beam
Probe beam
OG515
T
r

---
Calculate temperature profile in substrate
{partial T}over{partial z} = 0
Solve thermal diffusion equation assuming on the faces and T(r,z)=T0 on the rim (Substrate in heat sink).
Analytical solution exists:
nabla^2 T(r,z) = -{} {2 %alpha P}over{%pi K w^2} exp left(-2 {r^2}over{w^2} right) exp(-%alpha z)
T(r,z)=-sum from{n=1} to{infinity} {{4 %alpha P}over{%pi K R^2 w^2}} {int from{0} to{R} exp left(-{}{2 r'^2}over{w^2}right)J_0 left( {k_n r'}over R right)r' dr' }over{(J_0(k_n))^2} J_0 left( k_n r over R right) f_n(z) + T_0
f_n(z)= 1 over {%alpha^2 - left( k_n over R right)^2} left lbrace {%alpha R}over{k_n} left ( {e^ left(left( {k_n}over{R}-%alpha right)L right)-1}over{e^ left({2 k_n L}over{R} right)-1} e^ left( {k_n z}over R right) -{e^ left(-left( {k_n}over{R}+%alpha right)L right)-1}over{e^ -left({2 k_n L}over{R} right)-1} e^ left( {k_n z}over R right) right) right rbrace

---
3D - Temperature profile
For 4 W heating beam with 3.6 mm radius
Calculated on grid with 460 radial and 1000 axial steps

---
Evaluating the effects of the
temperature profile
Change of optical path length
OPL(r)=left( {nitalic{d}n}over{nitalic{d}T} + %alpha_T(n-1) right)int from{0} to{L} %DELTA T(r,z) nitalic dz
GRIN lens
Propagate a Gaussian beam with this OPL
alignl u(r,z)=u_probe(r,z) func exp left ( -i k OPL(r) right )newline phantom {u(r,z)} =u_probe(r,z) func exp left ( -i k left ( OPL(0) + OPL''(0){r^2}over{2} + O(r^4) right ) right )
Compare with propagation through a thin lens
u(r,z)=u_probe(r,z) func exp left ( i k r^2 over 2 1 over f right )
f = - {1}over{OPL''}
→ focal length

---
Calculated optical path length
Comparison with “ideal” thin lens (f = 1.88 m)

---
Measurement setup - beam analysis

---
Changes in Gaussian Mode
DCC LIGO-G050422-00-Z

---
Corresponding focal power changes
Focal power - diopters

---
Measurement setup - mode quality
Use optical cavity as mode reference
Look for introduced aberrations

---
Higher order mode content (normalized to TEM00)
 fixed mode-
matching lenses
 re-optimized mode- matching lenses
 Bull's eye (Laguerre-Gauss)
 Sum of other modes
 Hermite-Gauss 01/10
 Theoretical prediction

---
Conclusion
Excellent agreement with theoretical model
Technique is “touch free” and vacuum compatible
An aberration free lens can be created if:
  - The amount of heat is kept below the structural limit
  - The ratio of heating beam to probe beam radii is
    sufficiently large

---
Future work
Future work
Use different absorbing material
  - CO2 laser and fused silica
Start beam shaping experiments