## Slide 1: Study of Optical Scatterers within Coating Layers of gravitational wave detector Mirrors
L. Glover(1,3), R. DeSalvo(1,3), B. Kells(2), I. Pinto(3)
E. Arriaga(1), E. Barragan(1) E. Do(1), C. Fajardo(1), M. Goff(1), J. Patel(1), T. Sadecki(2), R. Savage(2), E. Villarama(1)
Related doc: LIGO-G1600431
1 – Cal State LA 2 – LIGO
3 – Uni. Sannio

## Slide 2: Gravitational Wave detectors’ mirror thermal noise
Dielectric coatings on mirrors present an anomalously low quality factor 104-105 as compared to >109 for Q-factor for the fused silica substrate.
This dissipation is responsible for most of the thermal noise of mirrors of all gravitational wave detectors.
Mechanical dissipation in coatings is the single most important limit for the detection range of Gravitational waves
Nobody knows where these losses reside or come from.

## Slide 3: Brief Summary
We analyzed scattering points in photos of Advanced LIGO mirror illuminated by 100 kW stored beams
Hundreds of thousands of progressively weaker scatterers were observed where few were expected, likely extending through the depths of the coating layer stack
Probable locus of the energy losses

## Slide 4: Method
Individual scatterers were identified using DAOPHOT an astronomer’s algorithm to identify stars in galaxies
Extract apparent amplitude and position of each scatterer
Subtract the identified “stars” and iterate

## Slide 5: Daophot Mechanism: Point Spread Templates
A point spread template is created from selected sources within the image.
Then it is used to search scatterers
Point Spread Template for an exposure time of 1.25 x 10-4 s

## Slide 6: Daophot Mechanism: Problems CCD dynamic range
Good
Badly saturated

## Slide 7: Daophot subtraction effectiveness
Pixel amplitude histogram of original Image
Residual pixel amplitude histogram after scatterer extraction
Most pixels restored to “dark” pixel
Residual pixel distribution within 2-3 pixels FWHM
Mostly from saturation effects
100
200
50
-50
Notes: Note for you, the central pixel does not count because it is just the black background that daophot ignores, but this is log scale, ignoring the central pixel you get 2-3 pixel FWHM

## Slide 8: Identifying/subtracting scatterers
dots mark the place where scatterers have been excised
“dirt” does not fit template is ignored by daophot and masks out real weaker scatteres
Original Photo
256
256
100
Subtracted Photo
Dark pixels
expanded pixel scale
Fluffy dirt
ignored

## Slide 9: Number of Scatterers vs. Exposure Time
Number increases almost linearly with exposure
Exploring weaker and weaker scatterers
Deeper and deeper in the dielectric coating layers ! !
Exposure Scatterers (1st Run)
@ 0.125 ms 76
@ 1 ms exposure 624
  @ 400 ms exposure 127,774
Scatterer count plateaus due to saturation.
100,000
10,000
1,000
100

## Slide 10: Apparent size: Depth in stack effect
There are two depth attenuation components:
Attenuation of impinging light due to reflections through depth of coating layers
Back-reflection on front layers attenuates Scattered light
Scattered light detected by CCD
Image: Stuart Reid, Iain Martin, 2016
Back reflected scattered light

## Slide 11: Scatterer light intensity distribution @ Exposure Time = 0.0125 sec
6000
3000
1000
5000
The rapid slope of reconstructed scatterers at low amplitude is compatible with what expected from the reflection curve.
Integrated CCD count

## Slide 12: Drop of laser light impedes detection of scatterers below first 2-3 layers 26 layers in each HR coating ~200 scatterers /mm2
How many scatterers
are actually there ?

## Slide 13: Origin of scatterers
Virtually no absorption (<0.25 ppm)
Positive or negative density (n) fluctuations
Positive = crystallites, in glasses catalyze crystallization
Negative = large fluctuation of natural voids in glasses
Both have dangling bonds, i.e. double well potentials adsorbing mechanical energy

## Slide 14: Ongoing work
Two steps proposed:
Sum coherently lower exposure images from LIGO to mitigate saturation.
Study ad-LIGO witness samples to determine scatterer’s depth distribution through layers and size distribution

## Slide 15: Lucky byproduct
  Study of image to image “star” position motion for coherent addition of images yielded a metod to independently detect:
Motion of stored beam within mirror
Motion of mirror w.r.t. camera.

## Slide 16
DAOPHOT position resolution
The scatter of the points (standard deviation) =
~11µm
positioning error of “daophot”
Calibration 1Pixel = ~80 µm
Differential “star” position between two images

## Slide 17
Detection of mirror motion
Mirror motion
Mirror position resolution ~ 1.3 µm
Calibration 1Pixel = ~80 µm

## Slide 18: Depth scatterer exploration
Study a spare witness samples to determine
the scatterer’s depth distribution
the scatterer’s size distribution

## Slide 19
1
3
2
50% Reflector
@ 45°
AdLIGO Multi-Layered Mirror
CCD Camera
Microscope
lens
White light LED
X, Y Axis micropositioning
Z Axis piezo focusing

## Slide 20
Grid scan of Mirror
X1
X2
…
Xn
Y1
Y2
Yn
…
Raster scan X-Y of microscope frames on mirror surface to identify rough scatterer position
Defocused
Scatterers

## Slide 21
  Depth of field 0.6 µm / n
  depth resolution of ~ 30 nm/ n achieved from Z-scan
  Wide angle-white light illumination allow penetration of many layers
Potential depth resolution
+Z
-Z
Maximum Luminosity
Defocused
Scatterer
Defocused
Scatterer
Focused
Scatterer
Notes: For your information, n is the refraction index of the material, in Ta2O5 or TiO2 it is between 2.5 and 3

## Slide 22: Conclusions 1
A very large population of scatterers was found on aLIGO mirrors under high-power illumination.
They contribute to large angle optical scattering,
if the observed points are the locus of mechanical dissipation, they may explain the anomalous mechanical dissipation observed in sputtered coatings.
The discovery is a good diagnostic tool, perhaps indicating possible ways to reduce the Sensitivity limitation for Gravitational Wave detectors

## Slide 23: Conclusions 2
Methods are being developed to monitor
mirror to camera and
beam to mirror
micro-movements
Both can be valuable diagnostic tools at the observatory