## Slide 1: Optical properties of SIlicon for cryogenic Gw detectors
Zeno Tornasi
11/07/2017 - Hilton hotel, Pasadena, ca, U.S.A.
LIGO-G1700998
R. Adhikari1, A. Bell2, R. Birney3, M. Fejer4, D. Gibson3, E. Gustafson1, J. Hough2, A. Markosyan4, I. W. Martin2, J. Steinlechner2,5, S. Reid3, S. Rowan2, S. Sproules2
1Caltech, 2UofG, 3UWS, 4Stanford, 5Hamburg

## Slide 2
Topics
Crystalline silicon
Optical scattering
                Amorphous silicon coatings
                Optical absorption

## Slide 3
Introduction
Why silicon?

## Slide 4
Noise in a gravitational wave detector
The LIGO Collaboration, Class. Quantum Grav. 32 (2015) 074001

## Slide 5
Noise in a gravitational wave detector
Coating Brownian noise
The LIGO Collaboration, Class. Quantum Grav. 32 (2015) 074001

## Slide 6
Noise in a gravitational wave detector
The LIGO Collaboration, Class. Quantum Grav. 32 (2015) 074001
Coating Brownian noise

## Slide 7
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)

## Slide 8
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
Limited room for improvement
Substrate engineering constraints

## Slide 9
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
Property of the coating material
Not much to do about it

## Slide 10
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
High refractive index materials

## Slide 11
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
Property of the material
Can vary by orders of magnitude
Can be engineered to some extent

## Slide 12
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
Current detectors operate at room T
Can we just go cryogenic then? Not yet…

## Slide 13
Fused silica has a high mechanical loss at low T
In general

## Slide 14
Fused silica has a high mechanical loss at low T
In general

## Slide 15
Fused silica has a high mechanical loss at low T
Currently LIGO optics are made of fused SiO2
In general

## Slide 16
Fused silica has a high mechanical loss at low T
Currently LIGO optics are made of fused SiO2
Since the ’50s we know that mechanical loss in SiO2 goes like →→
In general
Travasso F. et al. (2007) Europhys. Lett. 80 50008

## Slide 17
THE PROBLEM
Fused silica is used
As a substrate
As a coating
With tantala (also lossy at low T)
What do we use instead?

## Slide 18
Coatings: Amorphous silicon looks promising
SiO2
aSi
X. Liu, F. Hellman, et al, PRL 113, 025503 (2014)

## Slide 19
Coatings: Amorphous silicon looks promising
SiO2
aSi
Bonus
High refractive index
n = 3.47 @ 1550 nm helps reducing thickness
X. Liu, F. Hellman, et al, PRL 113, 025503 (2014)

## Slide 20
Substrates: Crystalline silicon looks great too
We know since the ‘70s that cSi has very low mechanical loss at low temperature.
Christopher Wipf / LIGO-G1700602
Credits: Ronny Nawrodt

## Slide 21
Recap
Both cSi and aSi have low mechanical loss at low temperature
But what about optical properties?
 | cSi (bulk) | cSi (surface) | aSi
Absorption | Bell, A. Markosyan | Ongoing (A. Bell) | This work
Scattering | This work | Future work? | Future work

## Slide 22
Crystalline silicon

## Slide 23
Crystalline silicon bulk absorption
Standard Czochralski grown silicon (Cz Si)
    Too impure for application in GW detectors
    because of high optical absorption
Float-zone silicon (FZ Si)
  Very pure and low absorbing: 2 ppm/cm @ 1550 nm
  Available in crystals of maximum diameter 20 cm
Magnetic field-grown Czochralski silicon (MCz Si)
  Available up to 45 cm in diameter
  Bulk absorption can be as low as 5 ppm/cm @ 1550 nm, albeit inhomogeneous
A. Markosyan, A. Bell / LIGO-G1700480
Surface absorption is a different beast
A. Bell / LIGO-P1700134

## Slide 24
Why scattering matters
Photons scattered
off axis
Add phase noise if they are reflected back in the system by the environment
Contribute to cavity round trip loss
Easily disrupt squeezed states

## Slide 25
The Glasgow scatterometer
Polariser

## Slide 26
The Glasgow scatterometer
Polariser

## Slide 27
The Glasgow scatterometer
Polariser
Direct calibration attempted shining the laser itself at the camera

## Slide 28
“Engineering run 1”: looking at CCl4

## Slide 29
“Engineering run 1”: looking at CCl4

## Slide 30
“Engineering run 1”: looking at CCl4

## Slide 31
2.6x105
“Engineering run 1”: looking at CCl4

## Slide 32
2.6x105
“Engineering run 1”: looking at CCl4
Very lumpy beam despite centrifuging and filtering through 0.2 μm filters
The peaks sit on a baseline
Obtained scattering ratio 3.5x larger than the value in literature

## Slide 33
Heraeus Suprasil 3001
fused silica cylinder
(same silica used in aLIGO)
“Engineering run 2”: fused silica

## Slide 34
Heraeus Suprasil 3001
fused silica cylinder
(same silica used in aLIGO)
“Engineering run 2”: fused silica
Bulk silica cylinder viewed face-on
Beam in the medium and its reflections

## Slide 35
Heraeus Suprasil 3001
fused silica cylinder
(same silica used in aLIGO)
Difference between direct calibration and CCl4
Scattering ratio obtained is 2.16x larger than literature, according to my direct calibration
Or it’s 0.6x literature, taking CCl4 as a reference
“Engineering run 2”: fused silica
Bulk silica cylinder viewed face-on
Beam in the medium and its reflections

## Slide 36
Heraeus Suprasil 3001
fused silica cylinder
(same silica used in aLIGO)
Difference between direct calibration and CCl4
Scattering ratio obtained is 2.16x larger than literature, according to my direct calibration
Or it’s 0.6x literature, taking CCl4 as a reference
Take away message
Still “commissioning” the scatterometer, plenty of things to understand better
BUT
2. It’s NOT off by orders of magnitude!
“Engineering run 2”: fused silica
Bulk silica cylinder viewed face-on
Beam in the medium and its reflections

## Slide 37
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab
Bulk MCz slab viewed face-on
Beam in the medium and its reflections

## Slide 38
Difficult to isolate the main beam from the many strong reflections (high refr. index, small polished sample)
Images 10 times brighter than fused silica under similar conditions.
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab
Bulk MCz slab viewed face-on
Beam in the medium and its reflections

## Slide 39
Difficult to isolate the main beam from the many strong reflections (high refr. index, small polished sample)
Images 10 times brighter than fused silica under similar conditions.
MCz Si scatters
at 1550 nm, at 16° observation angle:
0.11 - 0.17 ppm cm-1 sr-1
0.99 - 1.6 ppm cm-1
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab
Bulk MCz slab viewed face-on
Beam in the medium and its reflections

## Slide 40
Difficult to isolate the main beam from the many strong reflections (high refr. index, small polished sample)
Images 10 times brighter than fused silica under similar conditions.
MCz Si scatters
at 1550 nm, at 16° observation angle:
0.11 - 0.17 ppm cm-1 sr-1
0.99 - 1.6 ppm cm-1
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab
Bulk MCz slab viewed face-on
Beam in the medium and its reflections
45-74 ppm bulk scatter for a 46 cm thick test mass
No requirement in ET design document
Could be dominated by coating scattering*finesse

## Slide 41
Difficult to isolate the main beam from the many strong reflections (high refr. index, small polished sample)
Images 10 times brighter than fused silica under similar conditions.
MCz Si scatters
at 1550 nm, at 16° observation angle:
0.11 - 0.17 ppm cm-1 sr-1
0.99 - 1.6 ppm cm-1
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab
Bulk MCz slab viewed face-on
Beam in the medium and its reflections
45-74 ppm bulk scatter for a 46 cm thick test mass
No requirement in ET design document
Could be dominated by coating scattering*finesse
LIGO Core Optics Components Design Requirements Document

## Slide 42
Amorphous silicon

## Slide 43
Heat deposited aSi films made at UWS
Slides courtesy of prof. Stuart Reid

## Slide 44
Heat deposited aSi films made at UWS
Slides courtesy of prof. Stuart Reid
First coatings: 20 ppm/QWL
Very hard to reproduce!

## Slide 45
Description
Assuming aSi absorption 20 ppm/QWL at 1550nm
We need 5 bilayers of SiO2 and Ta2O5 to reduce the laser power
For an ITM with T= 6000 ppm we need 2 bilayers of SiO2 and aSi
For an ETM with T = 6 ppm we need 5 bilayers of SiO2 and aSi
Thermal noise improvement* compared to a pure SiO2 and Ta2O5 coating:
120 K 20 K ITM: -21% -20% ETM: -38% -36% total: -32% -31%
*Loss for aSi: values from commercial coatings; no cryogenic measurements on UWS coatings
Simulations: J. Steinlechner
Multimaterial coating with aSi

## Slide 46
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
Room temperature
deposition

## Slide 47
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
200 °C deposition

## Slide 48
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L)¦400 deg¦JGS1¦459nm | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 ¦400 deg¦7979¦548nm | 345.2424 | 327.7767 | 309.5171 | 347.9657
I16H0408 ¦400 deg¦7979¦548nm | 283.777 | 258.9255 | 256.9259 | 285.8381

## Slide 49
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L)¦400 deg¦JGS1¦459nm | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 ¦400 deg¦7979¦548nm | 345.2424 | 327.7767 | 309.5171 | 347.9657

## Slide 50
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L)¦400 deg¦JGS1¦459nm | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 ¦400 deg¦7979¦548nm | 345.2424 | 327.7767 | 309.5171 | 347.9657
400 °C – 3 hours

## Slide 51
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L)¦400 deg¦JGS1¦459nm | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 ¦400 deg¦7979¦548nm | 345.2424 | 327.7767 | 309.5171 | 347.9657
I16C3110(R)¦0 deg¦JGS1¦579nm | 898.1002 | 6849.2269 | 680.5181 | 1043.3642
I16E1708(L)¦200 deg¦JGS1¦242nm | 455.8398 | 390.4395 | 371.2299 | 481.4251
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16H0908 ¦0 deg¦7979¦636nm | 145.8385 | 131.9785 | 119.409 | 125.6444
I16H1107(R)¦200 deg¦7979¦523nm | 211.038 | 214.7153 | 227.1079 | 216.1971

## Slide 52
Deposition temperature - absorption correlation
Chart: Deposition temperature [°C]
| 0 | 0 | 0 | 0
I16C3110(R)¦0 deg¦JGS1¦579nm | 898.1002 | 6849.2269 | 680.5181 | 1043.3642
I16E1708(L)¦200 deg¦JGS1¦242nm | 455.8398 | 390.4395 | 371.2299 | 481.4251
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16H0908 ¦0 deg¦7979¦636nm | 145.8385 | 131.9785 | 119.409 | 125.6444
I16H1107(R)¦200 deg¦7979¦523nm | 211.038 | 214.7153 | 227.1079 | 216.1971
I16H0408 ¦400 deg¦7979¦548nm | 283.777 | 258.9255 | 256.9259 | 285.8381
I16C3110(R) | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L) | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L) | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H1107(R) | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R) | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 | 345.2424 | 327.7767 | 309.5171 | 347.9657

## Slide 53
Conclusions
Silicon is a promising material for cryogenic GW core optics.
It has low mechanical loss at low temperature, zeros of expansion coefficient, high refractive index
In Glasgow a scatterometer is active
It is able to take measurements to better than order of magnitude level but we’re working hard towards a fully reliable instrument
Preliminary measurement of MCz Si bulk scattering suggests that might be compatible with use in ET -- 45-74 ppm bulk scatter for a 46 cm thick test mass could be just as high as we can afford
Heat deposited aSi coatings show absorption comparable with annealed ones (but better mechanical loss).
A clear link has been established between absorption and dangling bonds, and absorption and deposition temperature.

## Slide 54
Thank you!

## Slide 55
Future
Optimise the scatterometer, understand its noise sources and discrepancies with literature
Carry out systematic angle-dependent measurements to verify to which extent the scattering observed is really only Rayleigh
Find a way to reliably calibrate the system
Work towards understanding surface absorption (not discussed here)
Integrate the aSi coatings study with other analyses such as Raman spectroscopy

## Slide 56
Photothermal common-path interferometry (PCI)

## Slide 57
EPR – Courtesy of Stephen Sproules

## Slide 58
EPR – Courtesy of Stephen Sproules

## Slide 59
Description
Simulations: J. Steinlechner
At 1064 nm RT:
We need 8 bilayers of SiO2 and Ta2O5 to reduce the laser power
For an ITM with T= 1.4% we can’t improve the coating using aSi in lower layers
For an ETM with T = 6 ppm we need 4 bilayers of SiO2 and aSi
Thermal noise improvement* compared to a pure SiO2/Ta2O5 coating:
Room temperature: ITM: - 0% ETM: - 28% total: -22%
Almost no improvement by reducing mechanical loss further (limited by silica loss and ITM thermal noise)
*Loss for aSi: values from commercial coatings; no cryogenic measurements on UWS coatings
EPR – Courtesy of Stephen Sproules
Notes: Jessica and Iain multimaterial idea