| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley |  | 06-04-18 | E1800167 | V1 | 06-05-18 |

Physical Configuration per D1800154-v2

100 ± 0.3 mm diameter right circular cylinder

10 ± 0.5 mm thick

Bevel for safety

Wedge  between 10 ± 5 arcmin

Material: Fused silica; Heraeus 311, 312, 313 or 3001

Registration mark: Arrow at minimum thickness. Chemical or laser etched, ground or sandblasted

Serial number “E1800006-xx” Chemical or laser etched, ground or sandblasted.  Number sequentially.

Surfaces, Sides and Bevel Polish

All Surfaces, Sides and Bevels shall be polished using a progression of smaller grit sizes.  The last step before final polish shall be equal to or less than a five micrometer grit finish. These surfaces shall appear transparent with no grey, scuffs or scratches visible to the naked eye when viewed in normal room light against a black background.

Scratches, Sleeks and Point defects according to MIL-PRF-13830B

Surface 1: 10/5

Surface 2: 60/40

Figure, measured over the central 95 mm diameter

Surface 1 and 2:  Nominally flat.  PVr < 100 nm

Error, High Spatial Frequency

< 1 Å rms