## Slide 1: Compare HWS measurements of current optics to transmission maps
Correlation between the transmission map and the HWS absorption map has been noted on ETM10, O3 LLO ETMx
The blue TM outline on the HWS data is approximate in all cases
  HWS maps stolen from G1900203
  Transmission maps cite DCC#
G. Billingsley, A. Brooks, L. Zhang

## Slide 2: Compare HWS measurements of current optics to transmission maps
 | ITMX | ITMY | ETMX | ETMY
L1 – abs status HWS Abs value Optic SN Trans. Map link | Uniform [0.6ppm] ITM04 https://dcc.ligo.org/E1200702 | Uniform [0.7-0.8ppm] ITM08 https://dcc.ligo.org/E1200575 | Point [0.1ppm] ETM10 https://dcc.ligo.org/E1500299 | Points 0.14 or 0.35ppm* ETM15 https://dcc.ligo.org/E1500301
H1 – abs status HWS Abs value Optic SN Trans. Map link | Uniform? [0.2-0.3ppm] ITM07 https://dcc.ligo.org/E1700232 | Point [0.26-0.36ppm] ITM11 https://dcc.ligo.org/E1400042 | Point [~0.25ppm] ETM13 https://dcc.ligo.org/E1500300 | Inconclusive [violates conservation of energy] ETM16 https://dcc.ligo.org/E1500302
L1
H1
https://ldas-jobs.ligo.caltech.edu/~aidan.brooks/
https://awiki.ligo-wa.caltech.edu/wiki/Auxillary_Optics_Stuff/TCSComponents/PreO3_Absorption_measurements
[Credit: LLO & LHO TCS teams]

## Slide 3: L1-ETMY surface deformation [scaled to same incident power]

## Slide 4: ITM04, O1, O2, O3 L1 ITMX

## Slide 6: ITM08, O1, O2, O3 L1 ITMY

## Slide 8: ETM10, O3 L1 ETMX

## Slide 10: L1 ETMY-ETM15

## Slide 12: ITM07 O2partial, O3 H1 ITMX

## Slide 14: ITM11, O1, O2, O3 H1 ITMY

## Slide 16: H1 ETMX – ETM13

## Slide 18: H1 ETMY-ETM16

## Slide 20: First observation: ITM03, 01,02 partial H1-ITMX
Removed after O2
Sent to CIT for forensics

## Slide 21: https://dcc.ligo.org/LIGO-E1400008